Afbeelding met tekst, gebouw, baksteen, bouwmateriaal

Automatisch gegenereerde beschrijving

# COLOUR

Black brown

# Product description

The bricks are formed individually in the unsanded mould to a solid mass, pressed from clay of alluvial origin from an area located in the Scheldt basin and fired in a tunnel oven at a temperature of approximately 1180°C. On the narrow side the bricks have an unsanded surface structure. The shape is slightly irregular. Finally the bricks are processed until they have acquired a weathered  
shape, due to which the paver surface leaves a rustic, aged impression.

# TECHNICAL CHARACTERISTICS

The paving is laid in fired clay bricks of Belgian origin, quality class A, carrying the CE and UKCA mark.

**CE label according to EN 1344 : 2013 / AC : 2015**

|  |  |  |
| --- | --- | --- |
| Manufacturing dimensions (L x W x H) | \*212x50x70 mm |  |
| Quantity / m² with a traditional joint | ca. 91 |  |

# PHYSICAL AND MECHANICAL PROPERTIES ACCORDING TO EN 1344: 2013 / AC: 2015

|  |  |  |  |
| --- | --- | --- | --- |
| **Aspect** | **Class** | **Mean** | **Individual** |
| Water absorption  NBN EN771 | W3 | Max 3% | Max 4% |
| Transverse breaking load | T4 | Min 80 N/mm | Min 64 N/mm |
| Abrasion resistance | A3 | Max 450 mm³ | Max 500 mm³ |
| Frost resistance | FP100 | freeze/thaw resistant | freeze/thaw resistant |
| Wet skid resistance | U3 | >55 |  |
| Acid resistance | C | < 7% |  |
| Size tolerance\* | NPD | NPD | NPD |

# Productshot

